At the present time diode-pumped solid-state lasers play an important role in industrial applications.  Especially for microdrilling, welding and cutting, high power lasers with good beam quality are needed.  Therefore, it is of major interest to solve problems such as thermal lensing and stress-induced fracture of rods occurring in high power solid-state lasers.  In solid-state lasers, part of the pump power is dissipated as heat, which is removed by external cooling of the active medium.  The resulting temperature gradient from the axis to the surface is responsible for the thermal effects in the active medium [1].  Basically, three optical effects contribute to the thermally induced lens:

- The change of the refractive index with temperature, dn/dT (thermal dispersion).

- Bending of the end faces due to the thermal expansion (end face effect).

- Stress induced birefringence.

The influences of the thermo-optical effects on the laser performance are:

- Limited stability range of the resonator.

- Changing beam properties with varying pump power.

- Reduction of the beam quality, (i.e. increase of M2 factor) due to phase distortions and the unfavourable ratio between laser rod and TEM00 mode diameter.

- The effects of depolarisation and bifocusing (leading to beam quality degradation).

Point (i) is the most critical issue in high-power lasers; together with (iii) one has either the choice of a narrow stability range with good beam quality or bad beam quality with a large stability range [2], see theory below for more details.

The complete compensation for the depolarisation has already been achieved [3], [4].  Solutions to compensate for the thermal lens with a convex mirror [5] or with negative lenses ground at the end of the rod [6,7] are optimised for a fixed power but do not extend the stability range.  The effect of the thermally induced lens can be reduced by using longitudinal cooling in a thin-disk shaped active medium but this technique is not suitable for materials with moderate absorption such as Nd: YAG [8], and still suffers from significant optical distortions at high powers [9].

The main problem with the compensation of the thermal lens is to maintain good compensation for the phase front distortions over a wide range of pump power.  Since the thermal lens in the laser rod changes with varying pump power, the compensating lens should adapt itself to these changes.  Recently, a self-adaptive scheme to balance the thermal lenses in laser resonators was presented in ref. [10].  An additional rod with negative temperature dependence of the refractive index is placed inside the resonator.  The heating of this compensating element through weak absorption of the intra-cavity power causes a negative thermal lens.  As the heating is from the laser itself, the lens is self-adaptive and if all the parameters are properly adjusted, it always ideally balances the positive lens in the laser rod.  As a more compact alternative, we here propose composite rods made of a transversally pumped Nd:YAG section sandwiched between two glass rods or vice versa, as shown in the figures 1 and 2.  In this situation the glass sections are heated by heat conduction through the YAG-glass interface and no absorption is required.  Therewith, the positive lens in the Nd:YAG section is balanced with the negative lens in the glass sections. Obviously, for a good compensation the compensating element should have strong negative dn/dT.  Moreover, the compensating element should have nearly the same expansion coefficient as the gain medium to overcome the problem of thermal stresses between the laser material and the compensating element.

For the investigations presented in this report, the finite element (FE) simulation was used to calculate the thermally induced optical path difference (OPD) and these results used to analyse the variation of the dioptric power of the induced thermal lens in the composite Nd:YAG – glass (PK51A) rods. Comparisons for different rod geometries and pump distributions are also presented.

Fig. 1 shows the first design, which we denoted as YGY. The compensating glass element is sandwiched between two pumped Nd:YAG rods.  Fig. 2 shows the second design denoted as GYG, where the Nd:YAG is sandwiched between two compensating glass elements.  In both designs the Nd:YAG section is pumped transversally.  A large variety of different powers and Nd:YAG-glass geometries have been investigated

Figure 2 Sketch of the design GYG.  LY is the length of the Nd:YAG crystal, LG is the length of the glass section and d is the diameter of the composite rod.

Figure 1 Sketch of the design YGY.  LY is the length of the Nd:YAG crystal, LG is the length of glass and d is the diameter of composite rod.

# Theory

# The thermally induced lenses

# In a solid-state laser, at least the energy difference between pump and laser photons is converted to heat.  A given heating distribution causes a corresponding temperature distribution Tx,y,z as determined by the heat conduction equation.  Cooling at the surface and heating in the material will lead to a temperature gradient and therewith to a heat flow.

The optical distortions produced in the laser rod are caused by the nonuniform temperature distributions in the laser. For a homogeneously heated rod of radius Rrod and length Lrod, with Lrod>>Rrod this temperature difference ΔT between the rod surface and the rod centre is given by [1]

ΔTrod=14π⋅KPheatLrod,                                                                                          (1)

where K is the thermal conductivity of the rod, and Pheat is the total power converted to heat.  This means, that for this special case the temperature difference between the rod surface and the rod centre does not depend on the radius but only on the heat dissipated per rod length.

The dioptric power from the thermal dispersion contribution is given by [1]:

Ddndt=dndt2⋅π⋅K⋅PheatRrod2                                                                                      (2)

The nonuniform temperature distribution also influences the mechanical behaviour of the material.  The thermally induced stress will produce changes of the refractive index due to the elasto-optic variation of the index of refraction.  The contribution to the dioptric power from the elasto-optic lens is given by [1]

Dr,φ=2⋅ΔTrod⋅LrodRrod2αexp⋅Cr,φ⋅n03,                                                                     (3)

where αexp is the thermal expansion coefficient of the rod, Cr,φ is the elasto-optic coefficient and no is the undisturbed refractive index.  The stress-induced lenses of eq. (3) depend on the local polarisation of the beam and lead to the so-called bifocussing effect.  In addition the stress-induced changes of the local refractive index leads to thermally induced depolarisation.

A further contribution to the total thermal lens is caused by the bending of the rod end faces due to its thermal expansion.  The extent of this so-called end-effect is about one rod radius with homogeneously heated rods.  This means that if the un-pumped region at the rod end is wider than one-rod radius, the rod expansion is the same for the whole cross-section.  For homogeneously pumped rods, the dioptric power of the end-effect is given by [1]

Dendeffect=αexp⋅n∘−1π⋅K⋅PheatLheat⋅Rrod.                                                                    (4)

Finally, if the resonator is long compared to the pumped laser rod, the various contributions to the thermal lens can be considered as closely spaced thin lenses and the total dioptric power of the rod is given by the sum of the individual lenses.  Neglecting the comparatively weak dioptric power of the stress-induced lens, the total dioptric power of the rod is

Dthermal=Ddndt+Dendeffect.                                                                                    (5)

Influence of thermal lens on the laser beam properties

The influences of the thermal lens on the laser beam have already been mentioned in the introduction.  In this section the relation of the power range and beam quality is discussed.

We start from the results published in the refs. [2, 11-12]: with increasing pump power, the changing focal length of the thermal lens in the gain medium modifies the laser modes and the stability of the resonator.  The resonator will be stable in a certain pump power range of width ΔP.  It is shown in ref. [2] that, apart of two exceptions (end-pumped and symmetrical resonators) a laser with a single thermal lens in the cavity has always two such stability ranges of equal width.  Within these two stable zones the radii of the modes at the location of the thermally induced lens vary significantly, being infinite at the edges of the stability ranges and having a minimum wmin somewhere in between.  In order to attain good beam quality, the Gaussian beam radius in the medium should be as large as possible. A general relation between the minimum of the fundamental mode radius wmin in the crystal rod and the range of the dioptric power ΔDtherm of the thermal lens for which the resonator is stable is given by ref. [2]:

ΔDtherm=2⋅λπ⋅wmin2,                                                                                              (6)

where λ is the wavelength of the laser mode.  In general, in a laser with one single thermal lens in the resonator, the radius of the fundamental modes reaches the minimum wmin twice, once in each of the two equal stable ranges.  However, if the thermal lens is located exactly in the centre between two identical mirrors, the gap between the two ranges of stability disappears [2,11].  The two stable zones merge and form the largest possible range of stability [13], given by

ΔDtherm=4⋅λπ⋅wmin2.                                                                                              (7)

In a first-order approximation, according to (2), (4) and (5), the dioptric power of the total thermal lens can be expressed in the form

Dtherm=Ppump⋅Dπ⋅wp2,                                                                                         (8)

where wp is the effective radius of the pumped region and D is a constant, which we call the specific dioptric power (mm2W−1m−1).  This specific dioptric power depends on the cooling method and on the material of the laser crystal.  With eq. (8) the two ranges ΔDtherm and the pump power range ΔP are linked as:

ΔDtherm=ΔPpump⋅Dπ⋅wp2,                                                                                     (9)

and inserting eq. (7), ΔP is found to be

ΔP=4⋅λ⋅wp2wmin2⋅D.                                                                                       (10)

Supposing that all transverse modes will oscillate whose beam radii are smaller then the radius of the pumped region, the beam propagation factor M2 can, to a good approximation, be calculated with (see the appendix)

M2=12⋅wpwmin2+12.                                                                                      (11)

By inserting eq. (10) into eq. (11) the beam quality factor can be expressed in the form

M2=18⋅ΔP⋅Dλ+12.                                                                                   (12)

The eq. (12) tells us that a large range of the pump power and a good beam quality cannot be achieved simultaneously without further measures.  In order to attain a large stability range with good beam quality the value of the total specific dioptric power D should be reduced.  This can be achieved by efficient compensation of the thermal lenses and this is the goal of the present work.  In both suggested composite rod designs, we will try to obtain a minimum value of the totalD of composite rods.

Processing of FE-code information

The composite rods under investigation in the present work cannot be modelled with the simple analytical method discussed in the previous section.  Due to the more complex structure of the composite rods under consideration and in order to get more detailed information about the thermal effects in these elements the numerical finite-element code SESES [14] was used.  In the first step SESES solves the three dimensional heat conduction equation (Poisson equation) in a laser rod containing a time independent heat source qx,y,z, the steady-state temperature distribution Tx,y,z reads [15,16]

∇2Tx,y,z+qx,y,zK(T)=0,                                                                              (13)

The boundary conditions to solve the equation (13) are given by Newton’s law of heat transfer

K⋅∂T∂N|s=h⋅Tc−Ts,                                                                                   (14)

where Tc is the coolant temperature which is assumed to be constant, Ts is the local

temperature on the rod surface s, N is the local normal to that surface and h is the heat transfer coefficient [17].

The finite element simulation program SESES [14] calculates the temperature distribution Tx,y,z and based on it the local displacement and the stresses in the crystal and the effect of the refractive index.

The optical path difference inside the laser rod

The optical path difference (OPD) is given by the phase shift suffered by the propagating light through the laser rod as compared to an undisturbed medium.  Due to the inhomogeneous temperature distribution, the OPD is a function of the transverse coordinates x and y (see fig. 3).  Following the references [18,19], the OPD for a beam passing in the z-direction (fig. 3) through a crystal of length l reads

OPDcalcx,y=0l∂n∂T⋅T(x,y,z)⋅dz+n∘−1⋅Δlx,y,                                        (15)

where the integral term containing the thermal dispersion n/T describes the contribution of the thermal part, i.e. the integrated refractive index change along a beam path parallel to the rod axis.  The term containing Δlx,y describes the end effect, i.e. the axial elongation of the crystal at the transverse point x,y and n∘is the undisturbed refractive index of the crystal.  In order to find the dioptric power

of the equivalent lens, the calculated OPDcalcr was fitted with a parabolical

OPDlensr.  The OPD of a spherical thin lens with a dioptric power D reads

OPDlensr=OPD0−12⋅r2⋅D,                                                                          (16)

wherer is the distance to the rod axis and OPD∘the optical path difference at r=0.

Y

Z

Rod axis

X

Figure 3 shows cylindrical coordinates of a laser rod.

[1] W. Koechner, “Solid- State Laser Engineering”, Series in Optical Science, Springer, Berlin, 1996.

[2] V Magni, “Resonator for solid-state lasers with large-volume fundamental mode and high alignment stability”, App Opt., 25 (1), January 1986, pp. 107-117.

[3] Q. Lü, N. Kugler, H.Weber, S. Dong, N.Müller and U.Wittrock, “A novel approach for compensation of birefringence in cylindrical Nd:YAG rods” Optical and Quantum Electronics, vol.28, pp.57-69, 1996.

[4] N.Kugler, H.Weber, S.Dong, N.Müller, U.Wittrok, “A novel approach for compensation of birefringence-compensation two-rod Nd:YAG laser system”, Applied Optics 36, 1997, 9359-9366.

[5] C. M. Stickley, “Laser Brightness, gain and mode control by compensation for thermal distortion, IEEE J.Quantum Electron.QE-2, 511 1996.

[6] L.M.Osternik and J.D.Foster,” Thermal effect and transverse mode control in a Nd:YAG laser,” Appl.Phys.Lett.12, 128 1968.

[7] F.A. Levie, “TEM enhancement in CW Nd:YAG by thermal lensing compensation,” IEEE J.Quantum Eelectron.QE-7, 170 1970.

[8] Y. Lion, R. J. D. Miller and M. R. Armstrong “Pressure tuning of thermal lensing for high-power scaling”, Optical Society of America vol.24, pp. 1343-1345,1999.

[9] Chr. Stewen, M. Larionov, A. Giesen, “Yb:YAG thin disk laser with 1 kW output power” ASSL conference 13-16 February 2000, Davos Congress Center, Davos, Switzerland.

[10] Thomas Graf, Rudolf Weber, Eduard Wyss, and Heins P. Weber, Photonic west, Conference on Laser Resonator III, 22-28 Jan.2000 San Jase, USA.

[11] K. P. Driedger, R. M. Iffländer and H. Weber, “Multirod resonator for high solid state lasers with improved beam quality” IEEE J.Quantum Electron.24 (4), 4 April 1988, 665-674.

[12] M.E. Innocenzi, Hura, C.L.Fincher and R.A. Fields,”Thermal moduling of contiuuous-wave end-pumped solid state lasers”, Appl. Phys. Lett. 56 (19), 7 May 1990,pp 1831-1833.

[13] Th.Graf, J. E. Balmer, R. Weber, H. P. Weber, “Multi-Nd:YAG-rod variable-configuration resonator (VCR) end pumped by multiple diode-laser bars” Optics Comm. 159 (1999) 83-87.

[14] Nm SESEStm (Semiconductor Sensor and actuator Simulation) is distributed by Numerical Modelling GmbH, c/o Winterthur Institute, Postfach, CH-8401 Winterthur, Switzerland.

[15] J. M. Eggleston, T. J. Kane, K. Kuhn, J. Unternahrer and R. L. Byer, “The slab geometry Laser-part 1: Theory”, IEEE J. Quant. Elecron. vol.20, no.3, pp. 289-301, march 1984.

[16] H. S.  Carlslaw and J. C. Jaeger, “Conduction of heat in solids”, 2nd ed., Oxford: Clarendon, 1989.

[17] W. Koechner, “ Absorbed pump power, Thermal profile and stresses in a cw pumped Nd:YAG crystal”, App. Opt., vol. 9, no. 6, pp. 1429-1434, June 1970.

[18] A. K. Cousins, “ Temperature and thermal stress scaling in finite-length end-pumped laser rods“, IEEE J. Quant Electron., vol.28, no.4, pp.997-1009, April 1992.

[19] C. Pfistner, R. Weber, H. P. Weber, S. Merazzi and R. Gruber, “Thermal beam distortions in end-pumped Nd:YAG, Nd: GSGG, and Nd:YLF rods“, IEEE J. Quant. Electron., vol.30, no. 7, pp.1605-1615, July 1994.

[20] D. C. Brown, “ Ultrahigh-Average Power Diode Pump nd:YAG and Yb:YAG lasers“ IEEE J. Quant Electron., vol. 33, pp. 861-873 (1957).

[21] Schott Glaswerke, Optische Glass, Hattenbergstrasse 10, W-6500 Mainz, Germany